## Slide 1
Machine learning for Catalysts Discovery: Application in CO2 conversion
Devis Di Tommaso
Department of Chemistry
School of Physical and Chemical Sciences
Queen Mary University of London

## Slide 2
CO2 utilization
Michael Barnard, Surrey Sustainable Engineering, 2024

## Slide 3
CO2 electrolysis and the sustainable carbon cycle
“Advanced Catalyst Design and Reactor Configuration Upgrade in Electrochemical CO2 Conversion”, Adv. Mater. 2023, 35, 2303052

## Slide 4
Electrocatalytic CO2 reduction
CO2
*COOH
*CO
PCET
PCET =
proton-coupled electron transfer
Pathways to C1 and C2 products
“Advanced Catalyst Design and Reactor Configuration Upgrade in Electrochemical CO2 Conversion”, Adv. Mater. 2023, 35, 2303052

## Slide 5
Electrocatalytic CO2 reduction
> 30 hydrocarbons, oxygenates
MAIN LIMITATION: Poor selectivity

## Slide 6
Quantum chemistry calculations of chemical reactions
, I = 1, N
Quantum mechanical
molecular energy
e-e
correlation
e-N
correlation
kinetic
term

## Slide 7
“Adsorption, activation, and conversion of CO2 on Cu–Sn nanoclusters”, Phys. Chem. Chem. Phys. 2023, 25, 13429
Quantum chemistry calculations of CO2 conversion

## Slide 8: Machine Learning in Catalysis
ML accelerated calculations to reach larger simulation cell size and time scales
ML potentials to achieve QC accuracy at a fraction of the cost
ML aided prediction of catalytic properties
Generation and analysis of data though through ML or training of ML methods
1
2

## Slide 9
Machine learning potentials
Active-learning scheme: unbiased and systematic selection of relevant training structures during ab initio MD  dynamically generated dataset
Jinnouchi et al., Phys. Rev. B 2019, 100, 0141 (implemented in VASP 6.3.0)
Atomic energy () function of the local environment
Potential energy
“short-range energy”

## Slide 10
Generation of amorphous models using MLFFs
Crystalline Cu (333)
Amorphous
Melt and quench using MLFF
MLPs trained and applied to model amorphous Cu-based alloys
Few hours with MLFF compared to weeks if done with DFT
“Impact of amorphous structure on CO2 electrocatalysis with Cu”, Electrochimica Acta 2024, 507, 145188
Screening CO2 activation on amorphous CuNi

## Slide 11: Machine Learning in Catalysis
ML accelerated calculations to reach larger simulation cell size and time scales
ML potentials to achieve QC accuracy at a fraction of the cost
ML aided prediction of catalytic properties
Generation and analysis of data though through ML or training of ML methods
1
2

## Slide 12: Molecular Graph Transformer
“Molecular graph transformer: stepping beyond ALIGNN into long-range interactions”, Digital Discovery 2023, 3, 1048-1057
MGT enhances material property prediction by integrating local and long-range interactions through advanced graph neural network architectures
MGT applied to the discovery of MOFs photocatalysts for CO2 reduction

## Slide 13
Key publications
  Unveiling Carbon Cluster Coating in Graphene CVD on MgO: Combining Machine Learning Force field and DFT Modeling, ACS Appl. Mater. Interfaces 2024
CO2 electrochemical reduction using amorphous catalysts: density functional theory and machine learning simulations, J. Energy Chem. 2025
  Molecular graph transformer: stepping beyond ALIGNN into long-range interactions, Digital Discovery 2024